ROOFING GUIDE SPECIFICATION PREPARED BY SIPLAST, INC.

PARAPRO ROOF MEMBRANE SYSTEM

NON-INSULATED – CONCRETE DECK

(NOTE:  This specification incorporates a Pro Base modified bitumen base ply.  Please contact Siplast Design Services for specifications with the Parapro Roof Membrane System applied directly to a concrete deck.)

This specification is provided as a general guide for use of Siplast, Inc. products based on typical building conditions and standard roofing practices. This guide specification is not a substitute for professional design services. The information in this guide specification must be reviewed/approved by a design professional and modified as necessary and appropriate for each project. Each project has unique requirements and Siplast, Inc. recommends that the Owner's representative independently verify the accuracy and appropriateness of the specification provided for a particular project. Each selection or deletion made to this guide specification should be carefully considered. Users of this guide specification assume sole responsibility for its use.

January 1, 2023

SECTION 07 56 00 – FLUID-APPLIED ROOFING

PART 1 - GENERAL

  - RELATED DOCUMENTS

- The project plans, details and general Contract requirements apply to this Section.

  - SUMMARY

- Items Included:

- SBS modified bituminous membrane roofing.

- PMMA Fluid-applied Roofing

- Walktread.

- Related Sections:

- Section 06 10 00 "Rough Carpentry" for wood nailers, curbs, and blocking, and for wood-based, structural-use roof deck panels.

- Section 06 16 00 "Sheathing" for wood-based, structural-use roof deck panels.

- Section 07 62 00 "Sheet Metal Flashing and Trim" for shop and field formed metal roof flashings and counter flashings.

- Section 07 71 00 "Roof Specialties" for factory fabricated metal copings, roof edge fascia, gravel stops, reglets, roof edge flashings, and counter flashings.

- Section 07 92 00 "Joint Sealants" for joint sealants, joint fillers, and joint preparation.

  - REFERENCES

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT STANDARD REFERENCES.

  - PREINSTALLATION MEETINGS

- Pre-installation Roofing Conference at Jobsite:  Hold a meeting with the Owner, Construction Manager, Architect, Roofing Contractor, Roofing Manufacturer's Representative, and other applicable trades to discuss the means and methods related to roofing installation.  The Roofing Contractor shall examine the substrate that will receive the specified roofing materials and confirm its suitability for attachment of the specified roofing system.

  - SUBMITTAL OF ALTERNATE SYSTEMS

- Consideration of Alternate Systems:  Submit primary roof systems to be considered as equals to the specified roof system no less than 10 days prior to bid date.  Primary roof systems which have been reviewed and accepted as equals to the specified roof system will be listed in an addendum prior to bid date; only then will equals be accepted at bidding.  Submittals shall include the following:

Identify fire rating in Item 4 below.

- Two 3 inch x 5 inch samples of the primary roofing and flashing membranes.

- Latest edition of the roofing system manufacturer's specifications and installation instructions.

- Evidence that the manufacturer of the proposed roofing system utilizes a quality management system that is ISO 9001 certified.  Documentation of ISO 9001 certification of foreign subsidiaries without domestic certification will not be accepted.

- Evidence of Underwriters' Laboratories Class [-----] acceptance of the proposed roofing system (including mopping asphalt or cold adhesive) without additional requirements for gravel or coatings.

- Evidence that the roof configuration (including fastening of insulation) has been tested by an accredited independent testing agency to meet the design wind load pressure indicated in Part 1.8 C2.

- List of 3 of the proposed primary roofing manufacturer's projects, located in the United States, of equal size and degree of difficulty which have been performing successfully for a period of at least 10 years.

- Sample copy of the proposed guarantee.

- Technical Product Data:  Submit the manufacturer’s technical product data sheets for each type of product.

- Shop Drawings:  Include plans, sections, and shop drawings/details for all applicable conditions.

- Product Samples:  Submit product samples of the specified base, finish, flashing reinforcing, and flashing membrane.

  - INFORMATIONAL SUBMITTALS

- Qualification Data:

- Installer:  Submit written confirmation that they have a minimum of 2 years of experience in successfully installing the same or similar roofing materials and be certified in writing by the roofing materials manufacturer to install the primary roofing products.

- Manufacturer:  Submit written confirmation that the manufacturer of the primary roofing products has been successfully producing the specified types of primary products for not less than 10 years with a consistent composition for a minimum of 5 years.

- System Qualification:

- Intent to Warrant Letter: Submit a signed letter on the roof membrane manufacturer’s letterhead, confirming that specified roofing system complies with the guarantee requirements indicated in Part 1.11 and the criteria indicated in Part 2.2 Roof Membrane Sheet Materials.

- Sample Guarantee:  Submit a sample copy of the manufacturer’s proposed Guarantee.

  - CLOSEOUT SUBMITTALS

- Maintenance Data: Submit the manufacturer’s care and maintenance guide.

- Executed Guarantee:  Provide the Owner with an executed version of the specified guarantee.

  - QUALITY ASSURANCE

- Fire Rating:  Submit evidence of exterior fire-test exposure by an approved third-party testing agency in accordance with ASTM E108 or UL 790 guidelines.

Indicate Class A, B, or C for the fire rating where the brackets appear in item 1 below.

- Class [----]

- Hail Rating:  Submit evidence by FM Global that the roof configuration has been tested to meet the following specified hail resistance design.

- Class 1-SH (severe hail) exposure.

- Wind Uplift Rating:  Submit evidence by an approved third-party testing agency that the roof configuration has been tested to meet the following specified wind uplift design.

Select item “1” for FM Global rated systems, or item “2” if using a different code approval agency or independent laboratory testing.  Indicate the wind uplift design criteria where the brackets appear.

- Class 1, 1-[----] windstorm construction.

- Minimum design wind load pressure of - [----] psf.

  - DELIVERY, STORAGE, AND HANDLING

- Delivery:  Deliver roofing materials to Project site in original containers with seals unbroken and labeled with manufacturer's name, product brand name and type, date of manufacture, approval or listing agency markings, and directions for storing and mixing with other components.

- Storage:  Store liquid materials in their original undamaged containers in a clean, dry, protected location and within the temperature range required by roofing manufacturer.

- Protect stored liquid material from direct sunlight, heat, open fire, ignition sources, oxidizing agents, strong acids, and strong alkalis.

- Discard and legally dispose of liquid material that cannot be applied within its stated shelf life.

- Protection:  Protect roof insulation materials from physical damage and from deterioration by sunlight, moisture, soiling, and other sources.  Comply with the insulation manufacturer's written instructions for handling, storing, and protecting materials during installation.

- Handling:  Handle and place roofing materials and equipment in a manner to avoid permanent deflection of deck.

  - FIELD CONDITIONS

- Weather Limitations: Proceed with installation only when existing and forecasted weather conditions permit roofing to be installed in accordance with manufacturer's written instructions and warranty requirements.

- Membrane Protection:  Provide protection against staining and mechanical damage for newly applied roofing and adjacent surfaces throughout this project.

- Debris Removal:  Remove all debris daily from the project site and take to a legal dumping area authorized to receive such materials.

- Site Condition:  Complete, to the owner's satisfaction, all job site clean-up including building interior, exterior and landscaping where affected by the construction.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT TORCH SAFTEY GUIDELINES.

  - GUARANTEE

- Manufacturer’s Guarantee: Provides that the Manufacturer will repair leaks through the covered roofing materials due to material or workmanship defects, subject to certain exclusions, during the specified time period. Refer to guarantee for complete coverage and restrictions.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT GUARANTEE COVERAGE.

- Special Project Warranty: Submit roofing contractor’s warranty signed by the Installer, including all components of the roofing and insulation system for the following warranty period:

      - Warranty Period: [---] years from date of Substantial Completion.

PART 2 - PRODUCTS

  - MANUFACTURERS

A.	Manufacturer: A roof system by the following manufacturer is approved for application.

- Siplast, Inc.

  - ROOFING MEMBRANE SHEET MATERIALS

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT BASE PLY.

- Resin for Finish Ply Membrane Construction:  A multi-component, fast-curing, flexible PMMA-based resin for use in combination with fleece fabric to form a monolithic, reinforced roofing membrane.  Physical and mechanical values are based on testing/evaluation of a 90-mil (2.3 mm) PMMA roof membrane reinforced with the specified fleece reinforcement.

- Thickness (avg):  90 mils (2.3 mm) at 0.31 kg/ft² (3.3 kg/m²) coverage rate (ASTM D5147, section 5).

- Peak Load (avg) @ 73°F (23C):  70 lbf/in (12.3 kN/m)  (ASTM D5147 section 6)

- Peak Load (avg) @ 73°F (23C):  90 lbf/inch (15.8 kN/m)  (ASTM D412, dumbbell)

- Elongation at Peak Load (avg) @ 73°F:  35% (ASTM D5147, section 6)

- Elongation at Peak Load (avg) @ 73°F:  35% (ASTM D412, dumbbell)

- Shore A Hardness (avg): 81 (ASTM D2240)

- Water Absorption, Method I (24h @ 73°F):  0.8% (ASTM D570)

- Water Absorption, Method II (48h @ 122°F):  1.2% (ASTM D570)

- Low temperature flexibility @ 23 F (-5°C):  PASS (ASTM D5147, section 11)

- Dimensional Stability (max):  0.15% (ASTM D5147, section 10)

- Tear Strength (avg):  90 lbf (0.4 kN) (ASTM D5147, section 7)

- Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

>	Parapro Roof Resin by Siplast, Inc.ºº

- Fleece for Membrane Reinforcement:  A non-woven, 110 g/m², needle-punched polyester fabric reinforcement as supplied by the membrane system manufacturer.

>	Pro Fleece by Siplast, Inc.

  - BASE FLASHING SHEET MATERIALS

- Stripping and Flashing Reinforcing Ply: An ASTM D6163, Type I, Grade S homogenous membrane with a glass-fiber reinforcing mat impregnated/saturated and coated each side with SBS modified bitumen blend with a factory applied polymer modified asphalt self-adhesive on the back surface of the sheet to provide full adhesion to the total surface area of the substrate.  The back side of the base ply shall be surfaced with a removable film, and the top of the sheet shall be surfaced with a factory-applied acrylic coating.

- Pro Base SA by Siplast, Inc.

- Liquid Flashing System:  The specified liquid flashing system shall consist of a catalyzed PMMA-based membrane fully reinforced with a non-woven polyester fleece that is installed over a prepared or primed substrate.

- Parapro 123 Flashing by Siplast, Inc.

  - BITUMINOUS MEMBRANE PRIMERS

- Asphalt Primer: Primer shall meet ASTM D41 criteria.

- PA-1125 Asphalt Primer by Siplast, Inc.

- Low VOC Asphalt Primer: Primer shall meet ASTM D41 criteria and South Coast Air Quality District and Ozone Transport Commission requirements.

- PA-917 Primer by Siplast, Inc.

- Primer for Self-Adhesive Membranes:  Primer for self-adhesive membranes shall be a single component, water-based resinous primer formulated to condition masonry, wood, plywood, concrete, asphaltic, and gypsum surfaces to facilitate adhesion of self-adhesive membranes.

- TA-119 Primer by Siplast, Inc.

  - AUXILIARY ROOFING MATERIALS

Delete auxiliary roofing materials listed below, as necessary, to meet individual project requirements.

- Roofing Asphalt: ASTM D312, Type [III or IV].

- Membrane Adhesive:  A single-component, moisture curing, low-odor adhesive designed for application of the specified roof membrane system.

- SFT Adhesive by Siplast, Inc.

Delete auxiliary roofing materials listed below, as necessary, to meet individual project requirements.

- Flashing Cement:  A single-component, moisture curing, low-odor adhesive formulated in a grade for application of flashing materials.

1.	SFT Cement by Siplast, Inc.

- Sealant:  A moisture-curing, self-leveling elastomeric sealant designed for roofing applications.

1.	PS-209 Elastomeric Sealant

- Sealant:  A moisture-curing, non-slumping elastomeric sealant designed for roofing applications.

- PS-715 NS Elastomeric Sealant

  - RESIN ACCESSORIES

- Cleaning Solution/Solvent:  A clear solvent used to clean and prepare transition areas of in-place catalyzed resin to receive subsequent coats of resin and to clean substrate materials to receive resin.

- Pro Prep by Siplast, Inc.

- Preparation Paste:  A PMMA-based paste used for remediation of depressions in substrate surfaces or other irregularities.

- Pro Paste Resin by Siplast, Inc.

- Repair Mortar:  A two-component, PMMA-based, aggregate filled mortar used for patching concrete substrates.

- Pro Mortar by Siplast, Inc.

- Thixotropic Agent:  A liquid additive used to increase the viscosity of the PMMA-based resin products, allowing the resins to be applied over sloped substrates.

- Pro Thixo by Siplast, Inc.

- Color Finish Resin:  A pigmented, PMMA-based resin for used to provide a color finish for both field and flashing membranes.

- Pro Color Finish by Siplast, Inc.

- Catalyst:  A peroxide-based reactive agent used to induce curing of PMMA-based resins.

- Pro Catalyst Powder by Siplast, Inc.

- Pro Catalyst Liquid by Siplast, Inc.

- Primers for PMMA Resin-based Roof Membrane and Flashing

- Primer for Wood, Plywood and Rigid Insulation, Masonry and Vertical Concrete Substrates:  A fast-curing PMMA-based primer for use in over wood, plywood and rigid insulation substrates.

>	Pro Primer W by Siplast, Inc.

- Accessories

- Ceramic Granule Anti-Skid Surfacing:  No. 11 grade specification ceramic granules suitable for broadcast into a PMMA-based resin wearing layer.

>	No. 11 Granules by Siplast

- Glass Beads:  A natural-colored glass bead for broadcast into the color finish layer of the waterproofing system to generate a skid resistant surface.  Glass beads shall be supplied by the manufacturer of the waterproofing membrane.

>	Pro Texture Beads by Siplast, Inc.

- Joint Tape:  A thermoplastic/rubber based sheet having a woven polyester backing used to treat joints between rigid insulation, flashing substrate panels and joints at cover plates used over sheet metal components.  The tape shall have a minimum width of 4 inches.

- Eternabond Webseal by Eternabond, Inc.

- Spray Primer for Stainless Steel, Aluminum and Copper Substrates:  An enamel spray primer for metal substrates to receive PMMA-based flashings.

- Rust-Oleum™ High Performance V2100 System Enamel Spray Primer by Rust-Oleum™, Vernon Hills, IL

PART 3 - EXECUTION

  - EXAMINATION

- Substrate Qualification:  The installing contractor shall examine all substrates where the specified roofing and flashing system will be applied and confirm their suitability to receive the specified roofing materials.

  - PREPARATION

- Sweep or vacuum all surfaces, removing all loose aggregate and foreign substances prior to commencement of roofing.

Keep item B if specifying a tear-off, partial tear-off, or re-cover.  Delete numbered conditions, as necessary to match project conditions.

- Remove all of the following existing conditions:

- Surface gravel

- Roof membrane

- Insulation

- Base flashings

- Edge metal

- Flanged metal flashings

- Cants

- Walkways

- Nonfunctional penetrations/curbs

- Drain assemblies

- Vapor retarder

- Metal trim, counter flashing

- Primer for Self-Adhesive Flashing Reinforcing Ply:  Apply the specified tacky primer by roller or spray in an even film. Refer to the manufacturer’s literature for the approved rate of application over various substrate types. Allow the primer to dry until it leaves a slightly sticky surface without transfer when touched.  Cutting or alteration of the primer is not permitted.

- Asphaltic Primer for Modified Bituminous Sheets:  Prime metal and concrete and masonry surfaces with a uniform coating of the specified asphalt primer according to the manufacturer’s published application rate.  Cutting or alteration of the primer is not permitted.

- Preparation of Steel Substrates:  Grind to generate a "bright metal" surface and remove loose particles.  Extend preparation area a minimum of 1/2-inch (13 mm) beyond the termination of the roofing/flashing system.  Notch steel surfaces to provide a rust-stop where detailed.

- Preparation of Stainless Steel, Aluminum and Copper Substrates:  Hand tool (SSPC-SP-2) or power tool (SSPC-SP-3) clean to remove loose rust, mill scale, and deteriorated previous coatings as well as to generate a tooth. Protect surrounding surfaces from overspray. Shake can for one minute after mixing ball is heard. Hold can 10-14 inches from surface. Apply several light coats a few minutes apart to avoid drips and runs. Recoat within 1 hour or after 24 hours; allow more time in cooler temperatures.  Monitor ambient and substrate temperatures/conditions to ensure that they are within the paint manufacturer’s acceptable range.

- Rigid Plastic Flashing Substrates:  Evaluate the plastic for compatibility with the resin materials.  Lightly abrade the surface to receive the flashing system, clean plastic substrates using the specified the cleaner/solvent and allow to dry.  Extend the preparation area a minimum of 1/2 inch (13 mm) beyond the termination of the flashing system.

- Preparation of Wood/Plywood Flashing Substrates to receive Resin:  Prime wood/plywood surfaces to receive the specified flashing system with the specified PMMA-based primer at the rate specified by the resin manufacturer and allow primer to cure.  Tape the joints between plywood or wood panels using gaffer’s tape prior to application of the lashing system.

  - INSTALLATION OF ROOFING, GENERAL GUIDLEINES

Keep items A and B, as appropriate, for cold adhesive and/or hot asphalt application.

- Asphalt Heating and Application:  Do not heat asphalt to or above its flash point.  Avoid heating at or above the FBT, should conditions make this impractical, heating must be no more than 25ºF  below the EVT and no more than 25ºF above EVT.  Follow the asphalt manufacturer’s published maximum heating temperature and minimum application temperature guidelines.  Ensure that all moppings do not exceed a maximum of 25 lb/sq.  Mopping shall be total in coverage, leaving no breaks or voids.

- Adhesive Application:  Apply membrane cold adhesive by roller, squeegee or spray unit in a smooth, even, continuous layer without breaks or voids.  Utilize an application rate for each ply as published by the roof membrane manufacturer.  Double the adhesive application rate at the end laps of granule surfaced sheets.  Where solvent-based adhesive is applied, refer to the manufacturer’s inter-ply flashing detail at the locations that are to receive the specified catalyzed acrylic resin primer/flashing system.  Cutting or alteration of the adhesive is not permitted.

- General Appearance:  Ensure that the finished roofing application has an aesthetically pleasing overall appearance and is acceptable to the Owner.

  - APPLICATION OF BITUMINOUS ROOFING MEMBRANE

Select parallel or perpendicular sheet orientation in Item A below.  Select application method for membrane plies below.

- Apply the modified bitumen ply sheet with side laps running [parallel/perpendicular] to the direction of the slope.  Exert sufficient pressure on the roll during application to ensure prevention of air pockets, wrinkles, creases or fishmouths.  Refer to the manufacturer’s guidelines for maximum sheet lengths and special fastening of the head laps where the roof deck slope exceeds 1/2 inch per foot.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT BASE PLY APPLICATION METHODS TO MEET THE SPECIFIED REQUIREMENTS.

  - APPLICATION OF BITUMINOUS STRIPPING

- Apply the specified base flashing materials in accordance with the manufacturer’s standard details.  Notify the design team immediately of any flashing heights below 8 inches.  Flash walls and curbs using the reinforcing sheet.  Exert pressure on the flashing reinforcing sheet during application to ensure complete contact with the vertical/horizontal surfaces, preventing air pockets.  Check and seal all loose laps and edges.  Nail the top edge of the flashing reinforcing on 9 inch centers.  Install the specified liquid-applied flashing system in accordance with the membrane system manufacturer’s printed installer’s guidelines and other applicable written recommendations as provided by the manufacturer. (See the manufacturer's schematic for visual interpretation).

  - MIXING OF RESIN PRODUCTS

- Preparation/Mixing/Catalyzing Resin Products:  Pour the desired quantity of resin into a clean container and using a spiral mixer or mixing paddle, stir the liquid for the time period specified by the resin manufacturer.  Calculate the amount of catalyst powder or liquid needed using the manufacturer's guidelines and add the pre-measured catalyst to the resin component.  Mix again for the time period specified by the resin manufacturer, ensuring that the product is free from swirls and bubbles.  To avoid aeration, do not use a spiral mixer unless the spiral section of the mixer can be fully contained in the liquid during the mixing process.  Mix only enough product to ensure that it can be applied before pot life expires.

- Preparation/Mixing/Catalyzing Aggregate-Filled Resin Products:  Pour the entire desired quantity of resin into a clean container and slowly add the pre-measured quantity of aggregate using a spiral mixer or mixing paddle, stirring the mixture for the time period specified by the resin manufacturer.  Calculate the amount of catalyst powder or liquid needed using the manufacturer's guidelines and add the pre-measured catalyst to the resin/aggregate mixture.  Mix again for the time period specified by the resin manufacturer, ensuring that the product is free from swirls and bubbles.  To avoid aeration, do not use a spiral mixer unless the spiral section of the mixer can be fully contained in the liquid during the mixing process.  Mix only enough product to ensure that it can be applied before pot life expires.

  - PREPARATION PASTE AND PRIMER APPLICATION

- Primer Application:  Apply catalyzed primer resin using a roller or brush at the rate specified by the primer manufacturer over qualified and prepared substrates.  Apply primer resin at the increased rate specified by the primer manufacturer over DensDeck Prime or other porous substrates.  Do not let resin pool or pond.  Do not under-apply or over-apply primers as this may interfere with proper primer catalyzation.  Make allowances for waste, including saturation of roller covers and application equipment.

- Paste Application:  Apply catalyzed preparation paste using a trowel over prepared and primed substrates.  Before application of any resin product over cured paste, wipe the surface of the paste using the specified cleaner/solvent and allow to dry.  Treat the surface again if not followed up by resin application within 60 minutes.

  - FLASHING AND FIELD MEMBRANE APPLICATION

- Base Flashing Application

- Using masking tape, mask the perimeter of the area to receive the flashing system.  Apply resin primer to substrates requiring additional preparation and allow primer to cure.

- Pre-cut fleece to ensure a proper fit at transitions and corners prior to membrane application.

- Apply an even, generous base coat of flashing resin to prepared surfaces using a roller at the rate specified by the resin manufacturer.  Work the fleece into the wet, catalyzed resin using a brush or roller to fully embed the fleece in the resin and remove trapped air.  Lap fleece layers a minimum of 2 inch (5 cm) and apply an additional coat of catalyzed resin between layers of overlapping fleece.  Again using a roller, apply an even top coat of catalyzed resin immediately following embedment of the fleece at the rate specified by the resin manufacturer, ensuring that the fleece is fully saturated.  Ensure that the flashing resin is applied to extend beyond the fleece (maximum ¼-inch (6 mm). Remove the tape before the catalyzed resin cures.  Make allowances for waste, including saturation of roller covers and application equipment.

- Should work be interrupted for more than 12 hours or the surface of the cured resin becomes dirty or contaminated by the elements, wipe the surface to be lapped with new flashing resin using the specified cleaner/solvent.  Allow the surface to dry for a minimum 20 minutes and a maximum 60 minutes before continuing work.

- Field Membrane Application

- Using the specified cleaner/solvent, wipe flashing membrane surfaces to be lapped with field membrane.  Allow the surface to dry for a minimum 20 minutes before continuing work.

- Apply an even, generous base coat of field membrane resin to prepared surfaces using a roller at the rate specified by the resin manufacturer.  Work the fleece into the wet, catalyzed resin using a 9-inch roller to fully embed the fleece in the resin and remove trapped air.  Lap fleece layers a minimum of 2 inch (5 cm) and apply an additional coat of catalyzed resin between layers of overlapping fleece.  Again using a roller, apply an even top coat of catalyzed resin immediately following embedment of the fleece at the rate specified by the resin manufacturer, ensuring that the fleece is fully saturated.  Make allowances for waste, including saturation of roller covers and application equipment.  Allow 2 hours cure time prior to exposing the membrane to foot traffic.

- Color Finish Application

- Ensure that the field and flashing membrane and has been in place for a minimum 2 hours.  Using the specified cleaner/solvent, wipe field membrane surfaces to receive the color finish layer.  Allow the surface to dry for a minimum 20 minutes before continuing work.

- Apply an even top coat of catalyzed color finish resin at the rate specified by the resin manufacturer.  Allow 2 hours cure time prior to exposing the membrane to foot traffic.

  - APPLICATION OF SEALANT

- Apply a smooth continuous bead of the specified sealant at the exposed finish ply edge transition to metal flashings incorporated into the roof system.

  - APPLICATION OF WALKTREAD

- Granule Anti-Skid Application:  Mask the areas to receive the anti-skid system using masking tape.  Apply an additional top coat of catalyzed roof resin at the rate specified by the resin manufacturer, immediately broadcast granules to refusal, and allow to cure.  Remove tape before the resin cures.  Allow 2 hours cure time prior to exposing the membrane to foot traffic.

- Glass Bead Anti-Skid Application:  Apply a layer of color finish using a prepared roof surface at the rate specified by the roofing system manufacturer.  Immediately broadcast glass beads into the wet color finish using a hopper gun at the rate specified by the waterproofing system manufacturer and backroll to embed the beads.

  - FIELD QUALITY CONTROL

- Notify the manufacturer of job completion in order to schedule a final inspection date.  Hold a meeting at the completion of the project, attended by all parties that were present at the pre-job conference.  A punch list of items required for completion shall be compiled by the manufacturer's representative.  Complete, sign, and send the punch list form to the manufacturer's headquarters.

- Leave all areas around job site free of debris, roofing materials, equipment and related items after completion of job.

- Complete all post installation procedures and meet the manufacturer's final endorsement for issuance of the specified guarantee.

END OF SECTION 07 56 00